2.4M PP SPUNBOND NONWOVEN PRODUCTION LINE

Ⅰ. Application:

This Produce line is filament polypropylene fiber spunbonded nonwoven fabrics equipment. Its raw material is polypropylene (PP), take the principle of spinning man-made fibers, during polymer filature, continuous filament is extended into fiber net, which is finished by mechanical hot pressing, The machine assembly we adopt is now advanced veneer integer slot air flow draw technology, the whole process from material feeding to cloth output is automatic control, short production flow, high working efficiency.

The nonwoven fabrics we produce has high strength, good softness, innocuity, bacterium-proof, corrosion resistance, high-level draw strength and elongation rate, They are widely used for dress, decoration materials, medical sanitation materials, daily life products and in the industrials, agriculture fields. In additional, this production line can produce nonwoven fabrics of different color, different grams, different lines according to users’ requirements.

Lines on nonwoven fabrics: dots, cross line, straight lines, weight:12-250g/m2

Raw material: Polypropylene chips

(melt index:20-40g/10min, melt point:166℃, ash content: ＜ 0.15-0.25%)

Ⅱ. Process flow:

Feeding(suction,dosing and mixing) →Melt and extruding(with recycle extruder)→Filtering→Metering→Spinning→Quenching→Air drawing→Forming→Calendering→Winding→Slitting→Product

Ⅲ Product specifications:

Installed power: 500KVA

Web width: 2400mm

Max. winding diameter: ф1000mm

Annual output: 2200tons/year

Single filament titer: ≤2.5 denier

Web weight: 12-250g/m2

Max. mechanical speed: 0-120m/min (Process speed:10-100m/min)

Electric consume: 800KWH/ton

Ⅳ. Workers and power

Number of workers: 3-4 persons

External power supply: 315KVA

Water system: 0.2Mpa

Ⅴ. Workshop requirement

L×W×H: 20×14×12.5m

Ⅵ Description of machine

- material feeding system

Max. feeding capacity: 500kg/h

Max. filling of Master batch: 10%

- Extruder

Diameter of screw: ф150mm

L/D: 30:1

Material: 38CrMoALA

Surface treatment: Nitriding and Polishing

Rotary speed: 20-70rpm

No. of heating zones: 6

Heater: Cast aluminum

Driving motor: Z4 90kw DC motor

3.  Edge recycle extruder

Diameter of screw: ф105mm

L/D:15:1

Material: 38CrMoALA

Surface treatment: Nitriding and Polishing

Rotary speed: 20-80rpm

No. of heating zones:3

Driving motor: 15kw AC motor

- Filter

Filter form: double-cylinder continuous switching

Equipment of Slurry coat: Forced seal structure

Filter area: 3.5m2×2

Suitable medium: Polymer melt

Rated flow: 500-700kg/h

Max. working pressure: 25Mpa

Max. working temperature: 310℃

Heating system: Heat conduction oil cyclic heating

Filtration precision: 50 micron

Size of filter elements: ф35×487mm .19pcs single cylinder

measurement pump

measurement capacity: 250cc/r

Rotation speed: 0-40rpm

Motor power: 5.5kw

- Spinning machine

Material of spinning head: 42CrMo

Attemperator: Heat conduction oil cyclic

Power of smoking machine:5.5kw

- Spinneret

Material: SUS431

Size: 2710×216mm,

Aperture: 45s

- Cross air blow Unit

Adopts Industrial air-conditioner quenching system

Power of air blower: 45kw

- Drawing unit

Adopts blow suction and stretching polypropylene filament yarn

Power of suction blower: 30kw

- Electric heater

Heat the conduction oil acquire constant temperature

Power: 48kw×2sets,  60kw×1set

- Calcinator

Heater adopts stainless steel heating pipe

Max. temperature: 550℃

- Ultrasonic cleaning machine

Cleaning mode: underfloor

Power of ultrasonic transmitter : 2400Wx2

Size of Internal groove: 3000×300×250mm

- Web former

Normal process speed: 10-100m/min

Motor power: 7.5kw DC motor

- Calender

Size of roller: ф460×2850mm

Working width: 2750mm

Product: ≥2400mm

Roller hardness

Engraved roller: HRC58

Plain roller: HRC60

Process speed: 10-100m/min

Transmission power:22kw, DC motor

- Winder

Process speed: 10-120m/min

Working width: 2400mm

Max. winding diameter: 1000mm

Roller changer: automatic moving knife

Motor power: 5.5kw

- Slitter

Max. mechanical speed: 300m/min

Working width: 2400mm

Motor power:4kw

- Refrigerating machinery

Refrigerating output: ≤35kw

- Electric control

SIEMENS PLC

10.4 inch touch screen

Inverter: FUJI(JAPAN)

AC contactor: Schneider(FRANCE)

Temperature control box: RKC

Ⅶ Other equipments

| Cooling tower | 1set |
| --- | --- |
| Electric Hoist | 1 set |
| Distribution panel | 1set |
| Spinneret | 1set |
| Climatic conditional cabinet | 1set |
| Air compressor | 1set |
| Pump | 1set |
| Professional tools | 1set |

Ⅷ Spare parts

| Dismantling tools for screw | 1set |
| --- | --- |
| Heat band of screw | 2sets |
| Platinum resistance | 3pcs |
| Electric equipment (low voltage) | several pcs |
| Filter screen of spinneret | 10pcs |
| Web curtain | 1pc (9X2.05m) |
| Filter O-rings | several pcs |

Ⅸ Buyer’s need to prepare the following thing:

Air pipe, water pipe, oil pipe and some related Moisture and heat preservation material

Air compressor pipe

Cable and cable tray

Water pool: 40m3

Electric balance: 0-200g

Normal tools: 1set

Lubricating oil and heat-transfer oil

Electric welding machine, gas cutting tools

Hoist:15t (used for temporarily erection)

Hydraulic car:3t

Chain hoist: 3t(2sets)

(Note: item IX are the things need buyer to prepare it, if anything change, the supplier will notify buyer)