COMPACT,21MPA MAXIMUM WORKING PRESSURE,ONE AND TWO STEEL

WIRE REINFORCED, RUBBER COVERED HYDRAULIC HOSE

● Tube:Oil resistant special synthetic rubber

Reinforcement:up to 1/2” one,from 5/8” to 1” two high tensile steel wire braids

Cover:Oil,abrasion and weather resistant synthetic rubber

Application:For medium pressure hydraulic systems in industry and agriculture

Temperature: -40℃~+121℃

● Characteristic:

Our hose passed ISO international SAE J517 test required,the impulse of our

SAE100R17 is up to 200,000 cycles

Service Life:2 years at least under right operation

Our hose has perfect performance when used in medium pressure systems on mobile and

stationary equipment.

- The superiority of our SAE100R17 is high quality with competitive price,which can help you to win larger market and more profit.

- Guarantee

- Package:The hose is packed by plastic film, exactly number of hoses is packed in the carton,wooden case available ,we can make the package as the customers requirements

Tips:

Age control of rubber hose is a method for designating a period of time,following manufacturer,during which ti is reasonable to expect that this products retains full capacities for rendering the intended.

Hose and hose assembly are affected by exposure to ozone,oxygen,heat,sunlight,rain and other similar environment factors. Storage of bulk hose should be in such a manner that exposure to these environment factors controlled as much as possible

| SIZE | I.D | REINFORCEMENT DIAMETER | O.D | W.P | B.P | BEND RADIUS | WEIGHT |
| --- | --- | --- | --- | --- | --- | --- | --- |
| INCH | DASH | MM | MM | MM | BAR | PSI | BAR | MM | KG/M |
| 1/4 | -4 | 6.2-7.0 | 10.4-11.1 | 12.5-13.3 | 210 | 3000 | 840 | 50 | 0.19 |
| 5/16 | -5 | 7.7-8.5 | 11.5-12.1 | 13.8-14.6 | 210 | 3000 | 840 | 55 | 0.22 |
| 3/8 | -6 | 9.3-10.1 | 14.0-14.6 | 16.2-17.0 | 210 | 3000 | 840 | 65 | 0.27 |
| 1/2 | -8 | 12.3-13.5 | 17.2-17.8 | 19.5-20.3 | 210 | 3000 | 840 | 90 | 0.46 |
| 5/8 | -10 | 15.5-16.7 | 22.0-22.6 | 24.3-25.1 | 210 | 3000 | 840 | 105 | 0.57 |
| 3/4 | -12 | 18.6-19.8 | 25.1-25.9 | 27.6-28.4 | 210 | 3000 | 840 | 125 | 0.78 |
| 1 | -16 | 25.0-26.4 | 32.6-33.4 | 35.2-36.0 | 210 | 3000 | 840 | 150 | 1.4 |