PVC /WPC Windowsill & Door Board Production Line

◆Processing Flow Chart

Wood-Powder           PVC Powder               Caco3                 Other Agents

Mixing according to certain Formula proportion

Extruding

Various PVC windowsill                             Various PVC/WPC Door Boards

The waste can be 100% recycled after crushed and milled

◆Workshop Composition & Needed Equipment

| NO. | Name | Equipment | Power | Quan | Application |
| --- | --- | --- | --- | --- | --- |
| 1 | Mixing Workshop | Mixing units(500/1000L) (with spiral feeder) | 75KW | 1 | Raw material mixture by formula, vibrating screen remove scum |
|  |  | SWP400 plastic crusher Crusher | 15KW | 1 | Break wastes into pieces |
|  |  | MF-500 High-Speed Plastic Mill | 37KW | 1 | Mill waste pieces into power for recycle |
| 2 | Extrusion Workshop | YF-800 PVC/WPC Wide Board Extrusion Line | 100 KW | 1 | Take mixed power into finial door board by extrusion device & moulds |
|  |  | Mould & die |  | 1 |  |
| 3 | Printing workshop | Laminating machine | 30KW | 1 | Surface treatment |

◆Machine Specification

1. Mixing units(500/1000L)

| 1. | Motor power | 47/67KW |
| --- | --- | --- |
| 2. | Hot Gross Capacity： | 500L |
| 3. | Hot Effective Volume： | 375L |
| 4. | Cool Gross Capacity： | 1000L |
| 5. | Cool Effective Volume： | 640L |
| 6 | Rotating Speed of Paddle ： | 413/830/71r/min |
| 7. | Heating Powder： | 9KW |
| 8. | Cooling Medium： | Water |
| 9. | Unloading Mode： | pneumatic |
| 10. | Weight： | 5.8TON |

2. SWP400 plastic crusher

| 1. | Crushing Capacity: | 350~450Kg/h |
| --- | --- | --- |
| 2. | Motor power: | 15KW |
| 3. | Spinning blade diameter: | 500mm |
| 4. | Spinning blade: | 5 pieces |
| 5. | Spinning blade rotation speed: | 500r/min |
| 6 | Dead knife quantity: | 2 |
| 7. | Sieve plate bore: | φ8~φ10mm |
| 8. | Feeding gate caliber: | 490×320mm |

3. MF-500 High-Speed Plastic Mill

| 1. | Capacity: | 80-120Kg/hr (PVC) |
| --- | --- | --- |
| 2. | Motor power: | 37KW |
| 3. | Fan power: | 3-5.5KW |
| 4. | Rated voltage/Nominal current: | 380V / 70.4amp |
| 5. | Rotational speed: | 4600r/min |
| 6 | Rotor number: | 3 |
| 7. | The milling room size: | 3720cm |
| 8. | The milling room diameter: | 400mm |
| 9. | Granularity: | 40-160item |

4. YF-800 PVC/WPC Wide Board Extrusion Line

This line consists of Spring feeder, Main extruder, Vacuum shaping tank, YF-800 haul-off, Cutter, Stacker.

- TS Series Plastic Spring Feeder

| Loading capacity | 150-300KG/H |
| --- | --- |
| Feed box volume | 150 L |
| Motor power | 1.5KW |
| Working angle | 35° |
| Spring Length | 5 meter |
| Stainless steel pipe | Φ 63 ×5m |
| Travel switch | ME8169 |

Note: The above parameters can be customized according to customer's requirements.

2) Main extruder －SJSZ80/156 Conical Twin Screw Extruder

| No. | Part name | Model and specification |
| --- | --- | --- |
|  |  | SJSZ80/156 | Quan | Remark |
| 1 | Capacity | 250kg/h~400kg/h |  |  |
| 2 | Screw | Diameter: Φ80/156 Material: 38CrMoA1A, Nitriding Nitriding layer Thickness: 0.4-0.6mm Surface rigidity:740-940HV Surface roughness: Ra ≤0.8um. Speed of Screw: 3-36rpm | 2 | Zhejiang Guangming |
| 3 | Barrel | Material: 38CrMoA1A, Nitriding Nitriding layer Thickness: 0.5-0.7mm Surface rigidity:940-1100HV Surface roughness: Ra ≤0.8um. | 1 | Zhejiang Guangming |
| 4 | Reducer Gearbox | SZ80 horizontal Gear Material: 20CrMoTi, Nitriding, Honing Reducer Motor: WB100-L2D-43 type, 1.5kw | 1 | Zhejiang |
| 5 | Distributor Case | Type: SZ80 Gear Material: 38CrMoA1A, Nitriding Axis Material: 40Cr Main Bearing: Wafangdian Bearing | 1 | Wuxi |
| 6 | Main driving motor | Y250L-4 type, 55kw | 1 | Suzhou Deneng |
| 7 | Main AC inverter | 3G3RV-ZV1 type, 55kw | 1 | YASKAMA(Japan) |
| 8 | Feeder AC Motor | VFD-007B, 0.75kw | 1 | Suzhou Deneng |
| 9 | Feeder AC inverter | VFD-007B type, 0.75kw | 1 | YASKAMA(Japan) |
| 10 | Barrel heating method | 18 heating zones; Cast-aluminum heating coil with the stainless steel shroud outside, 10.5kw | 6 | Jiangsu |
| 11 | Barrel cooling method | By air-cooled system DF4 , five pcs 0.25kw, one 0.37KW | 6 | Wuxi Teshun |
| 12 | Screw cooling method | Water cooling system |  | Jiangsu |
| 13 | Exhaust system | Water loop vacuum pump Motor: SZ-0.5 type,1.5KW Vacuum degree: -0.08Mpa | 1 | Ningbo Fangli |
| 14 | Temperature control meter | E5EZ-R3 | 10 | OMRON (Japan) |
| 15 | Thermocouple | K | 10 | Zhejiang |
| 16 | Tachometer | SX6 | 2 | Taiwan |
| 17 | Ampere meter | SX6 | 2 | Taiwan |
| 18 | General power air switch | DZ10-250A | 1 | Zhejiang zhengtai |
| 19 | Other air switch | 1P 2P 3P DE47-63 | 1 | Zhejiang zhengtai |
| 20 | Contactor | LC1 | 1 | Schneider(France) |
| 21 | Intermediate relay | HH54P | 1 | Fuji (Japan ) |
| 22 | Button, Indicator light | LAY | 1 | Schneider(France) |
| 23 | Axial-flow fan | YD150 | 1 | Jiangsu |
| 24 | Aviation plug | 16A | 7 | Suzhou yida |
| 25 | Aviation plug | WP2030A-2P | 6 | Weipu |
| 26 | Alarm system | Infrared monitor | 1 | Imported |
| 27 | Oil circulating system |  | 1 | Ningbo Fangli |

3) Vacuum shaping box

| Outer size: 4000*1100*1100mm, 304 Stainless steel material, brushed stainless steel plates panel and aluminum alloy rails. It can be adjusted in three-dimension direction, vertical moving by electric, horizontal moving by manual, and with a horizontal adjustment device. There are Vacuum 70pcs fittings , 70pcs water fittings with drying devices, and water consumption is 7m3/h. It also has four vacuum pumps(3sets 5.5KW and 1set 4KW) , one water pump (2.2KW ) and two air pumps (2sets 2.2 KW ). |
| --- |
| No. | Part name | Model and specification | Quan | Remark |
| 1 | Vacuum pump | 5.5kw | 3 | Fangli from Ningbo |
| 2 | Vacuum pump | 4kw | 1 | Fangli from Ningbo |
| 3 | Water pump | 2.2 kw | 1 | Chuanyuan from shanghai |
| 4 | Air pump | 2.2kw | 2 | Brand product |
| 5 | Reduction gears | Wpwko-60#-1/30 | 4 | Wuxi |
| 6 | Sealing bearing | 6208 | 8 | Brand product |
| 7 | Plain bearing | 51206 | 4 | Brand product |
| 8 | Vacuum meter | Z60-ZT | 4 | Schneider(France) |
| 9 | Vibration-proof Pressure gauge | 60M/M | 1 | Brand product |
| 10 | Air switch | 100A | 1 | Zhengtai(zhejiang) |
| 11 | alternating current contactor | LC1-D1810 D2510 D0910 | 7 | Schneider(France) |
| 12 | thermorelay | 9-13A 4-6A 2.5-4 | 6 | Schneider(France) |
| 13 | illuminated pushbutton | Red & green | 18 | Shanghai |
| 14 | data display instrument | UP5135 | 1 | Shenzhen |
| 15 | potentiometer | 10K | 1 | Changzhou |
| 16 | Fuse | JP5-2.5/RD | 1 | Shanghai |

4) YF-800 haul-off

| YF-800 tractor with draw type traction rubber blocks to make sure block replace easily ,The speed reducer gearbox and motor are from joint-venture brand company. Traction force is 10T, with speed of 0.7-2.5m/min, traction track length is 3 m, air pressure is 0.5-0.7Mpa. |
| --- |
| No. | Part name | Model and specification | Quan | Remark |
| 1 | Drive motor | WPDK070#20:1 | 2 | Zhejiang |
| 2 | Cylinder | QGB160*140-MF2 | 4 | Yongqing |
| 3 | reduction gears | BLY132-2.2KW | 2 | Wuxi |
| 4 | solenoid valve | 4V210-08 | 2 | Jiaerling |
| 5 | pressure regulating valve | AR2000 | 2 | Zhejiang |
| 6 | transducer | 5.5KW | 1 | YASKAWA(Japan) |
| 7 | scram | Y090-01ZS | 1 | Shanghai |
| 8 | contactor | LCI-D0901 | 2 | Schneider(France) |
| 9 | miniature circuit breaker | D20/3P | 1 | Schneider(France) |
| 10 | intermediate relay | HH54P | 1 | Schneider(France) |
| 11 | indicator light | Red & green | 2 | Shanghai |

- Cutter

| Motor power of 2.2KW , speed of 2,840R/min . Emery blades, diameter of 400mm, and with dust absorption device, air pressure of 0.5-0.7Mpa, cutting machine using a time relay, which is stable, reliable and easy to adjust , long free maintenance time. |
| --- |
| No. | Part name | Model and specification | Quan | Remark |
| 1 | Cylinder | SC80*1000-LB | 1 | Yongqing |
|  |  | SC80*900-LB | 1 | Yongqing |
|  |  | SC80*75-FA | 1 | Yongqing |
| 2 | Travel switch | YBLX-K3 | 3 | Shanghai |
| 3 | solenoid valve | 4V210-08 | 3 | Jiaerling |
| 4 | Sealing bearing | 6004 | 18 | Brand product |
| 5 | Cutting motor | YB65-2-2.2B5 | 1 | Longxin from wuxi |
| 6 | Alloy saw bit | ￠400 | 1 |  |
| 7 | Water treater | AC3010-03 | 1 | Brand product |
| 8 | Breaker | D20/3P | 1 | Schneider(France) |
| 9 | AC contactor | LC1-D0910 | 1 | Schneider(France) |
| 10 | Thermorelay | 4-6A | 1 | Schneider(France) |
| 11 | intermediate relay | HH54P | 4 | Schneider(France) |
| 12 | Digital relay | ST3PA-D | 1 | Schneider(France) |
| 13 | Digital time relay | JSS20-48AMS | 1 | Schneider(France) |
| 14 | Knob | Black | 1 | Shanghai |
| 15 | indicator light | Red & green | 2 | Shanghai |

- Automatic stacker

| stainless steel, Automatically air operated turning |
| --- |
| No. | Part name | Model and specification | Quan | Remark |
| 1 | Cylinder | 50×100CB | 2 | Yongqing |
| 2 | Solenoid valve | 5/2 way , 6102 | 1 | Yongqing |
| 3. | Travel switch | LXK3-20S/P | 1 | Shanghai |

- PVC/WPC door board & PVC Windowsill Mould & Die

| Mould Material | 38CrMoA1A |
| --- | --- |
| Inner Face | Hard chrome plating |

6.PVC windowsill & door board laminating machine

| Max Sheet width | 1300mm |
| --- | --- |
| sheet thickness | 2-50mm |
| sheet speed | 5-15m/min(可调) |
| total power | 32kw |
| pneumatic working pressure | 4kg |
| weight | 8000kg |

Note:

(1) All the measurement units of the gauge table is conformed to the GB standard. The whole equipments have one-year’s quality guarantee. After one year, the fittings will be supplied in a preferential price.

(2) The seller will assist the buyer to layout the workshop. The seller will send the technicians to test the machine in buyer’s workshop with buyer’s confirmation.

WUXI SENJIE PLASTIC MACHINERY CO., LTD

Address: NO.61 Renmin East Road, Yangshi Luoshe Town, Wuxi City, Jiangsu, China.

Tel: 0086-510-8021 9119   Mobile: 0086 13915229945   Fax: 0086-510-8021 9159

Attn: Sherry Wang   E-mail: wxsenjie@gmail.com  Website: www.sjsjcn.cn