Quotation

We supply SLW--1200 Single Layer Stretch Film Machine Production Line, the newest information as follow:

Ⅰ.Feature:

1. It profits advanced technology from aboard and manufacture by absorption, improvement, innovation.

2. It is entire frequency conversion control, movement stable, highly effective and the low energy consumption.

3. The product adopts the craft of one time forming.

4. It can produce two-side sticks for stretching film, cling film.

Ⅱ. Unit introduction

1. This series unit is mainly used in producing the polyethylene plastic film for unidirectional stretch (stretching film, twines membrane) as well as fresh film.

2. Therefore it applies in building material, hardware fitting packing widely. The screw of unit adopts 38CRNOALA alloy steel. It manufactured by nitric and precise processing so that it is highly hardness and durable long time.

3. Temperature controls adopts advanced automatic control system and the T mold adopts the multi- spots adjustment. They could cause the film thickness to be evener.

4. The cooling system adopts the circulating water cool and it cooling effect is good.

5. The rollout installment adopts the friction type of rollout and has the cutting edge installment and side material rollout element by round-trip. This causes the film which rollout to be neater.

Ⅲ. Main Technical Parameter

| Model | SLW-1200 |
| --- | --- |
| Screw Diameter | 70mm |
| L/D ratio | 28:1 |
| Screw Barrel Material | 38CRMOLA |
| Die width | 1450mm |
| Film Width | 1200mm, 600×2, 400×3 |
| Thickness | 0.008-0.05mm |
| Rollout Diameter | 400mm |
| Max. output | 80kg/h |
| Main Motor Power | 18.5kw |
| Heating Power | 25kw |
| Overall dimension: | 6000×2000×2500mm |
| Total Weight | 4000kg |

| Standard configuration |
| --- |
| Item | Description | quantity |
| 1 | Automatic Winding changer | 1pcs |
| 2 | Inverter | 1set |
| 3 | Automatic Trimming device | 1pcs |
| 4 | Automatic Temperature Control | 12unit |
| 5 | Step Motor | 1set |
| 6 | AC Motor | 1set |
| 7 | Gear box | 1set |
| 8 | Panel box | 1set |
| 9 | Switch (ZHENGTAI) | Several pcs |
| 10 | Electrical component (ZHENGTAI) | Several pcs |
| 11 | Hopper | 1pcs |
| 12 | Cooling roll (diameter: 270mm) | 2pcs |
| 13 | Air compressor | 1pcs |

| Accessories |
| --- |
| Item | Description | Quantity |
| 1 | Tools | 1pcs |
| 2 | Instructions | 1pcs |
| 3 | Schematic | 1pcs |
| 4 | Current meter | 1pcs |
| 5 | Voltage meter | 1pcs |
| 6 | Thermocouple | 1pcs |
| 7 | Relay |
| 8 | Main electrical components |
| 9 | Button switch |

Ⅳ. Quotation (F.O.B Price to Ningbo port)

| Model | Price |
| --- | --- |
| SLW-1200 single layer | 25450USD |

Our price valid period last for 2 months.

Ⅴ.Delivery

Within 30 days shipment the machine，we manufacture the machine after we receipt 30% deposit.

Ⅵ.Guarantee

- One year guarantee the quality of machine. But the buyer need pay the cost of maintenance if it is break down due to incorrect operation.

- Spare parts attached for free, problem parts can be changed for free in 1 year, but the express fee should be paid by users, others(if needed) suggest to be bought at the first time to save the cost of transportation.

Ⅶ. Technical services

- We will teach your staff to learn all the operation instruction in our factory if needed, this operation is easy to learn and only 1 person is enough to control !

- If need our engineer go to your country or teach and install ,the flight fee, the living fee, engineer salary (80 USD/per day) should be in charge by buyer

- We would present buyer the specification and Video or CD along with the machine when shipment.

Ⅷ. Package

In wooden box, or stretch film package or in bulk just according to the situation of shipment or clients, wooden box need pay extra package charge.