AAC material active ingredients ayalysis-Fly Ash

(only for reference,the materials components could be change according fact )

| 1. Fly ash (粉煤灰)(65-70%) |
| --- |
| Index Item | Grade (%) |
|  | Ⅰ | Ⅱ |
| Degree of fineness | (0.045 square hole sieve left amount) ≤ | 30 | 45 |
|  | (0.080 square hole sieve left amount) ≤ | 15 | 25 |
| Ignition loss ≤ | 5.0 | 10.0 |
| SiO2 ≥ | 45-55 | 40 |
| SO3 ≤ | 1 | 2 |
| Reference : The fineness can choose 0.045 or 0.080 square hole sieve left amount judge |

| 2. Lime (石灰)(8-25%) |
| --- |
| Item | Grade |
|  | Super Grade | First Grade | Qualified product |
| A(CaO+MgO) Quality Fraction % | ≥ | 90 | 75 | 65 |
| MgO Quality Fraction % | ≤ | 2 | 5 | 8 |
| SiO2 Quality Fraction % | ≤ | 2 | 5 | 8 |
| CO2 Quality Fraction % | ≤ | 2 | 5 | 7 |
| Digestion speed ,min | ≤ | 5-15 |
| Digestion temperature , ℃ | ≥ | 60-90 |
| Undigested residue quality fraction ,% | ≤ | 5 | 10 | 15 |
| Fineness (0.080 square hole sieve left amount) % | ≤ | 10 | 15 | 20 |

| 3.Cement (%)(水泥)(6-15%) |
| --- |
| SiO2 | Al2O3 | Fe2O3 | CaO | MgO | C3S | C2S | C3A | C4AF |
| 21-23 | 5-7 | 3-5 | 64-48 | 4-5 | 44-59 | 18-30 | 5-12 | 10-18 |

| 4. Plaster（石膏）(3-5%) |
| --- |
| CaSO4 | ＞ | 70% |
| MgO | ＜ | 2% |
| Chloride（氯化物） | ＜ | 0.05% |
| Preferably ground residue 90µm（可接受残渣） | ＜ | 10-15% |

| 5. Aluminium power（铝粉）(about 0.08%) |
| --- |
| Type and recommendation for supply depend on raw materials and mix formula |
| Metal Content | Approx. | >=65% | Powder 铝粉 |