HS9600 Pentaerythritol triacrylate (PET3A)

1. Type: HS9600 is trifunctional acrylic ester UV curing activity monomer.

2. Physical data

| Appearance | Yellowish viscosity liquid |
| --- | --- |
| Color（Pt-Co）,≤ | 1 |
| Water content %，≤ | 0.2 |
| Acid value mgKOH/g，≤ | 0.5 |
| Viscosity mPa.s | 450-700 |
| Specific gravity | 1.09-1.12 |

3. Application character

a. High reaction, high Crosslink density.

b. Use in UV curing resin’s activity thinner and as the middle substance for

composing the polyurethane.

c.  Excellence compatible and attachment character.

4. Application

As the Activity thinner applying in,

a. ABS, PS, PC ect engieer plastic surface UV decorative and protective coating.

b. Steel, aluminum surface decorative and protective coating

c. Strength the attachment and resistance to grind in the UV paint

5.Solvent dilutedness

HS9600 can be compatible with the ester, ketone, and aether ester type Solvent, i And it also can be diluted by toluen the ethyl acetate, Butyl acetate, Acetone and IBA solvent. Please test the stability of resin in the

solvent and the effection to the paint film in the solvent.