Zinc Stearate APL-308

Description

Characteristics: Stable, transparent, polishment, dispersion, anti-deposition

Solvent degree: Zinc stearate cannot solve in the water, aether and ethanol, can solve in the high-temperature benzene, acid and general solvent.

Application :

It can be as the PVC stabilizer, sanding sealer varnish, use in the wooden varnish, plastic, macromolecule colophony, fibre rubber, cosmetic, powder metallurgy and cement products.

Package : 20Kg/bag

Loading：1*20 container, one container can be loaded for 11.5 tons without pallet, 11.2tons with pallet.

The chemical index :

| Item | Analyze result | Analyze area | Analyze method |
| --- | --- | --- | --- |
| Metal content (zinc)% | 10.98 | 10.0-11.2 | USP23 |
| Metal oxide (zinc oxide)% | 13.67 | 12.5-14.0 | USP23 |
| Water content% | 0.3 | Max 0.5 | Infrared |
| Free fatty acids% | 0.24 | Max1 | FCC111 |
| Melting degree | 123.8 | 120-128 | Melting point |
| Density G/L | 268 | 230-310 | In house |