Structural Silicone sealant for glass fish tank  (C-353)

TECHNICAL DATA SHEET

Characteristics:

- One component

2. Fast acid curing, high strength

3. Non-discoloring.

4. Excellent cohesion for super aquarium and glass and most building materials.

5. 100 % Imported WACKER

5. Excellent resistance to low and high temperature, little performance changes between -10 ℃~120 ℃

Application:

1. Joint sealing for high-grade glass assembling.

2. Joint sealing for day lighting roof construction and great glass

3. Joint sealing of side window and rear window glass

4. Joint sealing for super aquarium and tank

5. Assembly for various kinds of windows and doors.

6. General joint and seal

Limitations:

- Cannot be used as structural sealant.

- Not compatible with materials with grease or exudation.

- The construction surface should be clean and dry.

- Not applicable to the seal of the immersed, airtight, or comprising substrates like copper, brass and lead, and oil-exudation surfaces.

- Cannot be used on the substrate surface below 6℃ or above 40 ℃

Notices:

- For best result results, use opened cartridges on the same day. Otherwise store it strictly tightened

2. Pre-test is necessary to ensure the excellent adhesive property.

3. Avoid contacting with skin or eyes, in case of contacted, rinse immediately with plenty of water, go to hospital if necessary

4. Keep away from children before curing.

5. Avoid contaminating food, medicine or cosmetics.

Color available:

White, grey, transparent, others of special order

Curing Time:

Track-free Time is between 5-15 minutes at room temperature

Completely curing Time is between 24 hours to 72 hours at room temperature.

Packaging

Cartridge: 300 ml   24 cartridges/ctn

Gross weight: 340g     Net weight: 280g

Storage and transportation:

12 months stored in a dry and ventilated place below 27℃ in original packaging.

Non-dangerous, can be transported by train, automobile, ship.

- Testing Standard: GB/T 14683-2003

| No | Item | The standard | Test result |
| --- | --- | --- | --- |
| 1 | Appearance | Have no grain, no agglomerations, no skinning, and no bubble. | Pass the standard |
| 2 | Density (g/cm3) | ±0.1 | 0.980 |
| 3 | Droop degree （mm） | Uprightness | ≤3 | 0 |
|  |  | Level | No damage | No damage |
| 4 | Skinning time (h) | ≤3 | 0.2 |
| 5 | Elastic recovery ratio (%) | ≥80 | 99 |
| 6 | Extrusion ability( ml/min) | ≥80 | 108 |
| 7 | Tensile modulus (Mpa) | 23℃ | ≤ 0.4 | 0.39 |
| 8 | Cold-hot adhesive | No damage | No damage |
| 9 | Under water adhesive | No damage | No damage |
| 10 | UV radiation | No damage | No damage |
| 11 | Definite Elongation | No damage | No damage |