Quotation

Description                              Type                 Unit price

Plastic Laminating Machine              SJ-FMF90/1000            $28800

The above price is based on FOBwenzhou port china excluding installation charge and commision.

Laminating Machine

Making use of the good adhesive property of polypropylene & polyethylene at melting status, the machine adheres and laminates paper or color-printed OPP & CPP film to woven bag under pressure, and through cutting-off and sewing to make paper & plastic laminated or color-printed packaging woven bags.

The extruder, with helical gear reducer of 20CrMnTi alloy steel and the screw &cylinder made of nitrided 38CrMoA1A alloy steel adopts automatic temperature control system to adjust melting temperature. Width of coating & laminating can be regulated, and stepless speed regulation is to control coating thickness and laminating speed, 6 stations for material feeding. The pneumatic-hydraulic edge correction for rewinder assures the accuracy of coating.
Pneumatic roller can assure even pressure. Frictional winding device is equipped.

Main Technical Parameters:

| Model No. | SJ-FMF90/1000 |
| --- | --- |
| Diameter of Screw (mm) | 90 |
| L/D Ratio of Screw | 26:1 |
| Number of Die | 2 |
| Width of Die (mm) | 1000 |
| Gross Power (kw) | 58 |
| Motor Power of Extruder (kw) | 15 |
| Heating Power of Extruder (kw) | 32 |
| Power of Driving Motor (kw) | 5.5 |
| Max. Coating Width (mm) | 750 |
| Coating Speed (m/min) | 30-100 |
| Installing Dimensions (L×W×H) (mm) | 13800×6000×2500 |
| Approx. Weight (kg) | 8000 |

Note:

1. Part 3 stops production, the lamination machine only include part 1 and part 2.

2. Kraft or Bopp film can be laminated with PP fabric.