ANIKOM Co. Ltd.

Conformity Certificate

Product: Plastic Sheet (Geomembrane),

Batch №    19      Production date     12 июня  2014г.

Plastic sheet made from carbon black-stabilized low density polyethylene (HDPE) according to Regulation No. 2246-001-77066742-2012.

Quantity, sq. m.  17000  Thickness, mm  1,0    Width, m  5

Design: sheet

Test Results:

| № | Item | Requirements of Regulation No. 2246-001-77066742-2012 | Test Results |
| --- | --- | --- | --- |
| 1 | Geomembrane outside appearance | The surface of the geomembrane must be smooth, without cracks, tears, holes | The surface of the geomembrane is smooth, without cracks, tears, holes |
| 2 | Density at 20 ° C, kg / cu.m. | Not standardized | 940-960 |
| 3 | Tensile strength, MPa, not less - In the longitudinal direction - In the transverse direction | 25,0 23,0 | 26,2 24,1 |
| 4 | Breaking elongation,%, not less | 700 | 718 |
| 5 | Tear strength, N / mm - In the longitudinal direction - In the transverse direction | 250 300 | 270 320 |
| 6 | Water absorption,% by weight, when tested at least for 24h | No more than 2 | 0,0-0,1 |
| 7 | Chemical resistance | Resistant to acids (excluding concentrated nitric and sulfuric acid) and to various concentrations of alkalis | The material is resistant to chemicals |
| 8 | Waterproof for 72 hours at 20 ° C,% | Waterproof | Waterproof |
| 9 | Geomembrane thickness, um | 1000±10% | 980-1005 |
| 10 | Geomembrane width, mm | 5000±2% | 5000 |

Conclusion: Meets the requirements of Regulations № 2246-001-77066742-2012

Storage: stored in coils in enclosed dry place away from direct sunlight, in a horizontal position at tº from + 5ºC to + 40ºC

Guaranteed 1 year shelf life when stored properly

Director of Quality Control ______________________Шипицын А.В

Place Stamp Here

27.06.2014.