|  | PU isocyanate and polyol for shoe sole |
| --- | --- |
|  | HT-9890/F-2390 | Q/320581GNU 001-2012 |

- Features：ultra high hardness, super low density.

- Application：women sandals, high heels.

- Resin Character:

| name | appearance | viscosity （Pa·s/40℃） | density （g/cm³/40℃） | package（kg/drum） | valid period | Mix ratio： A/B=23/29（drum） |
| --- | --- | --- | --- | --- | --- | --- |
| HT-9890 | Liquid or wax | 1950±400 | 1.12~1.14 | 18 | 6 months |  |
| F-2390 | Liquid or wax | 500±200 | 1.18~1.20 | 20 | 3 months |  |

- Catalyst and assistant：

| name | HT-9890 | SM-2 | water | hardener |
| --- | --- | --- | --- | --- |
| amount | 18Kg | 280g | 130~150g | 600-1200g |
| Remark: the amount of catalyst and assistant will change in different environment. |

- molding condition and physical property：

| Reaction | Value | Test (6mm sample） | value |
| --- | --- | --- | --- |
| mix ratio（by weight） (HT+SM)/F | 100/120~140 | sole density（g/cm³） | 0.32-0.38 |
| resin temperature（℃） | A: 40-45 B: 35-40 | hardness | JISA | 90-95 |
|  |  |  | ASKER-C | / |
| cream time（s） | 6~8 | tensile strength（MPa） | 5.0~7.0 |
| rise time（s） | 9~16 | elongation（％） | / |
| Touchable time（s） | 20~25 | NBS abrasion | ≥10％ |
| Mold temperature （℃） | 55~60 | free foam density （g/cm³） | 0.15~0.18 |
| Demolding time （min） | 3~5 | flexing endurance | / |

●dissolution condition: HT-9890 is at 50~60℃，10±2 hours；F-2390 is at 50~70℃，20±4 hours。

●mix ratio is based on the best matching, the number will vary according to the assistant weight.

●Free foam density changes about 0.02 in different seasons (as humidity and temperature changes)

●If shoe soles’ density is low, you need to improve the mold temperature, meanwhile release time will be increased with the thickness of the molded article extended.

●以上数据仅作参考，具体数据以实际操作为准。如需其他物性指标，请与我公司技术人员联系。

The above data is for reference only, specific data subject to the actual operation . For additional physical properties, please contact our technical staff.