Glue Board

1. The glue board fly killer can be used instantly
2. On the basis of special chromatography, it is able to trap insects on the both sides, which greatly improves the effect.
3. With high durability, the flat board is resistant to sun exposure, rain and high temperature, without the risk of curl or ageing.

Suggestion: The product may be used in conjunction with our bug zapper and other products, which contributes to realizing complete insect control in a safe and efficient method.

Technical Parameters

1. Standard: GB/T 24689.4-2009
2. Made of PP, the glue board fly killer comes with good strength and hardness.
3. Thickness: 0.3-0.35mm
4. Specification: 30cm*25cm, 30cm*20cm, 25cm*20cm, 15cm*20cm customization
5. At the temperature of 10°C-70°C, the product does not readily deform, and its glue is not fluidities or dissolved in water. Even in bright sunshine, the colors of both sides are nearly the same as each other. A related inspection report can be provided. 
6. Color: Yellow, blue or customization 
7. Glue: Hot melting pressure-sensitive adhesive that is non-toxic and odorless, resisting acid, alkali, water and corrosion.
8. It is covered with glue on both sides, and the adhesive layers are even and uniform. The thickness of an adhesive layer is 0.03-0.05mm. Adhesive failure will not occur when you spilt the product.
9. Adhesive strength≥6.8*10-4N/mn2
10. With smooth surface, it has been bored holes for hanging.