Evaluation Only. Created with Aspose.Pdf. Copyright 2002-2014 Aspose Pty Ltd.

High Temperature HEPAFilter

Speciality:

Common Applications:  It  is  mainly  used in  the  areas  requiring high-temperature

purification equipments and systems of automobile manufacturing, hot air filtration in

high temperature  spraying environment,  food, pharmaceutical  and other  production

processes or the clean oven.

Features:  deep-pleat  structure, high  temperature  resistance  or  superfine  fiberglass

filter  paper as  the  media, high  temperature  sealant,  special aluminum  foil  as the

separator,  special  equipment   for  folding,  stainless   steel  as  the   framework,  its

efficiency is up to F9-H14.

Temperature resistance: 250℃ and 350℃

(Specification)：

Initial Resistance

Dimensions

Filter Area

Rated

（Pa）

Type

W*H*D

(mm)

(㎡)

Airflow

H10

H12

H13

H14

（m /h）

3

305*305*150

610*610*150

1220*610*150

320*320*220

484*484*220

630*630*220

305*610*292

610*610*292

2.4

10.2

20.6

4.1

250

1000

2000

350

SHW-HG

≤150

≤190

≤220

≤240

9.6

1000

1500

1000

2000

16.5

10.1

20.9

Note: Other specifications are available on request