XINXING ground mat type : Plastic ground mat , HDPE ground mat , plastic road mat ,temporary road ,lawn protection mats ,oil drilling rig mat ,drilling rig floor mat ,plastic ground mat ,construction road mat ,heavy duty access mat ,plastic access mat ,Temporary road mats ,construction road mats

Popular Size :4500X2000MM ,3000X1500MM ,3000X2500MM ,3000X2000MM

Loading weight : more than 300 ton

Life :more than 10 years life

Customer size :

4500X2000mm      3000X2000mm

6000X2000mm      3000X2500mm

Cleat Height :5mm on both sizes
Normal Connections
Thickness can be 20mm to 100mm
Min Loading weight : 180 tons
Material :PE composite material and recycled UHMWPE material

World Popular Color for Ground mats

Black ,white ,Dark green ,Yellow ,Red  and so on .Customer made color is also available with us .

Where can we use ground mats

●construction sites

●golf courses

●utilities and landscaping
●tree care
●cemeteries
●oil drilling industry
●Marsh , wet muddy ground condition

For more professional information ,please visit our website at www.xgroundmats .com

| Factor | Value |
| --- | --- |
|  | HDPE | UHMWPE 100% RE |
| Tensile Strength(MPa) | 22 | 25 |
| Notched Impacted Strength Kj/m2 | No break | No break |
| Elongation at break (%) | ＞100% | ＞50% |
| Acids-concentrated | Good--Fair | Good-Fair |
| Acids-dilute | Good | Good |
| Aromatic hydrocarbons | Fair | Fair |
| Greases and Oils | Good-Fair | Good-Fair |
| Halogenated Hydrocarbons | Fair-Poor | Fair-Poor |
| Halogens | Fair-Poor | Fair-Poor |
| Ketones | Good-Fair | Good-Fair |
| Alcohols | Good | Good |
| Alkalis | Good | Good |
| Density(g/cm） | 0.93-0.97 | 0.95-0.98 |
| Water absorption-over 24 hours (%) | ＜0.01 | ＜0.01 |
| Resistance to Ultra-violet | Poor | Poor |
| Radiation resistance | Fair | Fair |
| Dielectric constant@1MHz | 2.3-2.4 | 2.3 |
| Dielectric strength(KV/ mm) | 22 | 28 |
| Dissipation Factor@1MHz | 1-10*10 | 1-10*10 |
| Surface resistivity(Ohm/sq) | 10 | 10 |
| Volume resistivity(Ohm-cm) | 10-10 | 10 |