- Push Pull Double Screens Filter Without Mesh

  - Product Structure

Pictures are only for information, take practicality as standard.

This machine mainly includes 7 parts：box, oil cylinder,screen, scraper, automatic waste discharge valve,hydraulic station,electric box.

  - Technical Data

- Machine Parameters:

| Item | Screen Diameter | Mesh Size | Suitable Extruder | Suitable Plastic | Output Per Hour(kg) （depend on fresh material output） | Motor Power(kw) |
| --- | --- | --- | --- | --- | --- | --- |
| LN300 | Φ300 | 10,20,30,40,50,60,70 | Φ130-Φ160 | PP,PE,ABS,PS,PVC,PA | 250-600 | 2.2 |
| LN370 | Φ370 | 10,20,30,40,50,60,70 | Φ140-Φ180 | PP,PE,ABS,PS,PVC,PA | 350-800 | 2.2 |

（the output set depend on fresh material,output reduces 15%-20% for recycled material）

- Technical Data:

Item NO.:LN300 /LN370(with two screens&one scraper in it)

Discharge Waste Type:Gate Segment Automatic Type

Mesh Size: depend on our factory specifications

Screen Material:Imported special tool steel,surface heat treatment,hardness≧60

Scraper Material: H13,carbide welding

Box Material:P20

Reducer: Sanlian Brand

Electric Box:1 set,3 zone

Volts:380V,50HZ

- Working Principle

The material flow into filter after heating in the cylinder;screens filter impurities;scraper push up and down,blow away the impurities which can’t pass through screens.so make sure useful material pass through continually.useful material outflow from discharge gate,enter into next working unit;impirities is collected in waste valve,automatic timing open waste valve for discharging waste.

The machine has three heating zones, which are filter box heating, discharge port heating and waste discharge port heating to constant the temperature of the material. By the K type thermocouple to detect the district's temperature feedback to the temperature control table, the temperature control table to control the on-off of the solid state relay to adjust the temperature.

- Mesh Size

（2.0mm）

（1.5mm）

5 （1.2mm）

8 （1.1mm）

10 （1.0mm）

15 （0.9mm）

20 （0.8mm）

30 （0.7mm）

40 （0.6mm）

50 （0.5mm）

55 （0.4mm）

60 （0.3mm）

- Contact:Freda Xu

Email:fredaxu@hotmail.com

Mobile No./whatsapp:+86 15068654923

Wechat:xy845609040