YANCHENG KEBO HYDRAULIC MACHINERY CO.,LTD

### Model KB-125C Automatic Roof Tile Making Machine

#### Ⅰ.Technical data

| Roof dimension | 424×337mm |
| --- | --- |
| Forming speed | 7~8 pcs/min |
| Production capacity | 3500pcs/8 hours（424×337mm） |
| Forming | Press and sieve |
| Power | 14.45KW |
| Mainframe size (L×W×H) | 2700×1600×2480mm |
| Weight | 5000kg |

Ⅱ.Production Procedures

| raw material cement 1.4 medium sand 2.0 fly ash 0.6 |  | 1. scooper |  | 2. grind-ing mixer |  | 3. ratio-n mixer |  | 4、 tiles molding machine |  | 5、 cure pallets |  | 6、 cure rack |  | 7、 manually or automatic spraying line |  | finished tiles |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

- Moulding

Water will be got rid of during production, the pressure should be over 100tons((The pressure gauge indicates over 13MPa) and the pressing time should not be less than 3 seconds.

Change the filter net on lower mould in time, usually 2~3 times each shift. If water polluted and muddy, then filter net should be changed, otherwise tile’s quality will be affected.

2. Curing

Generally, wet tiles should be naturally cured 24 hours on the pallets, and humidity and temperature should be controlled at the same time. Take away pallets when tile surface solid, water tiles everyday in the first week, and water amount subject to humidity. It’s better to put tile in vertical way and 28- day curing time is needed before on sale

3. Color Painting

Color is painted after tile completely dried and dusted (water moisture content not over 2%). First painting for bottom layer with temperature range 50℃～60℃, after dried then paint the surface layer.

Ⅲ.Raw materials:

Raw materials should be mixed with grinding mixer for 5~10 mins. This production line is equipped with JLH-350 grinding mixer. ( exceeding capacity 350L, ￠1300mm, 12rpm)

| Raw materials | Specification | Ratio（kg） | Notes |
| --- | --- | --- | --- |
| Cement | P.O or P.S 32.5# | 50 |  |
| Sand | Medium sand，Mx=2.3～3.0 | 80～100 | ≤￠5mm |
| Additive | Water-reducing agent | 0.5～1.0 | optional |
| Fly ash | Should be qualified | 10～30 | optional |

Notes：

1.cement：sand = 1:1.5～2.0 （weight）

2.water : cement = 1:0.25～0.35. The water should not be too much, otherwise tile will stick to mould.

3.The quantity of clay or mud contain in raw materials should not be over 3%, otherwise quality will be affected.

4. The color used for spraying is called crylic acid

Ⅳ. Supporting Items:

1.Curing rack: 30 sets( each set holding 120 pcs, seller will provide drawings)

2.Workshop: 800m2, which including the curing area, raw material storage area

3.Installation time: 15 days ( including the time for worker training)

4. Operators (totally 8 persons/ shift)

| No. | Post | Operators |
| --- | --- | --- |
| 1 | {<}0{>MaimMoulding machine operation | 1 |
| {0><}0{>2<0} | Mixer supplying and operation | {0><}0{>1<0} |
| 3 | Moving wet products to tile rack | 2 |
| 4 | {0<}0{>Transiting green products into curing room<0} | 1 |
| 5 | Color painting | 1 |
| 6 | Tiles delivering and packing | 2 |

Ⅶ. Roof Tile Mould Introduction：Below mould designs for reference only, other roof tile moulds also could be produced according to buyer’s drawings.

- Double Roman Main Tile: commonly is made of steel

Steel Mould: upper mould is made of Cr12, lower mould made of S45 and mould frame is made of 40# steel

Steel pallet: 1.6mm thickness

2.	Roof tile accessories: commonly is made of plastic. Steel mould also could design if required by buyer.