Outdoor Emulsion Paint

| Type | Theory paint area | Luster | Scrubbable times | Operate | Proportion | Character |
| --- | --- | --- | --- | --- | --- | --- |
| W30 | 8-12m2/kg (plane surface, one time, 30 micron) |  | More than 80000 times | The wall to be painted should be dry, and there is no powder, mildew or algae. The PH value of wall surface should be below 10. Operators should first paint a layer of Haisun solvent alkali-resistant primer WD3 on the wall, then paint the finishing coating for at least two times according to the proportioning. Roller coating, spray coating and brush coating are all available. | Paint: special diluents = 100:20-30 | Haisun W30 series exterior wall paint is easy to be painted and fast dry. The wall painted by Haisun exterior wall paint has matt film, elegant color and smooth hand feeling. The paint film has high hardness and tenacity. The exterior wall paint has the features of strong covering power, low viscosity, good weatherproof performance, strong hydrophobic nature, good extensibility, good self-cleaning property, and strong resistance to alkali and acid. It can make up and cover the fine crack automatically. Service life: more than 10 years. |