Steps of Concrete Floor Polishing

1.   Leveling—Level the uneven and rough surface with diamond pads, grits:30#  (if your concrete floor is hard ,you can use 20# first step)

Recommend pads model as follows:

2T-2  20# 30# 60# 80# 150# 300#

2. Hard Crystallization treatment :Apply the concrete harden agent  XY-103 to the floor till it is dry then forward to the next step

3. Rough grinding —— Apply 2T-2 to remove marks left after leveling, grits: 80# 150# 300# one by one

4.Fine polishing——Apply polishing pads 4FSZ/BTD-3.5 to fine polishing, remove marks left after rough grinding, improve the brightness of concrete, grits: 30# 50# 100# 200# 400# 800# 1500# 3000# .

Recommend super concrete polishing pads as follows:

4FSZ/BTD-3.5  the dry pads grits(30# 50# 100# 200# 400# 800# 1500# 3000#)

Or wet polishing pads 088-4B